Figure 1 Thermogravimetric analyses for the Ni samples.

Figure 2 H2-TPR analyses for the Ni samples.

Figure 3 X-ray diffraction patterns of the fresh Ni samples and the γ-Al2O3 support.

Figure 4 TEM images of the fresh (a, b) Niinc, and (c, d) Niwet samples.

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Figure 5 (a) N2-physisorption isotherms, and (b) Pore size distribution of the fresh Ni/γ-Al2O3 samples

Figure 6 Catalytic performances of the Ni catalysts in function of time of reaction.

Figure 7 Time-on stream product selectivity in glycerol conversion over (a) Niinc and (b) Niwet

Figure 8 Infrared spectra of reduced Ni catalysts after evacuation of CO.

Figure 9 Raman spectra of the used Ni catalysts.

Table 1 Textural and physical-chemical properties of fresh Ni catalysts and γ-Al2O3 support.

| Sample | SBET (m2/g) | Pore volume (cm3/g) |  | Pore size (nm) | NH3-TPD (µmol/gsample) | Number of exposed Ni atoms |
| --- | --- | --- | --- | --- | --- | --- |
| -Al2O3 | 113 | 0,20 | 4,54 |  | 182,1 | - |
| Niinc | 99 | 0,17 | 4,54 |  | 205,4 | 3,43 x 1019 (33%)a |
| Niwet | 108 | 0,17 | 4,15 |  | 224,5 | 9,22 x 1019 (82 %)a |